## Slide 1
THE
FACULTY OF
ENGINEERING
www.strath.ac.uk/engineering
X THE PLACE OF USEFUL LEARNING

## Slide 2
Atomistic Simulations of Polymers for Sustainable Food Packaging Design
Nisha Middleton
MDAnalysis UGM
Sep 2023

## Slide 3
Plastic Film Packaging
Multilayer components
Nearly 1/4 of UK consumer plastic1
Only 7% currently recycled in UK1
Increases shelf life of food
Increasing demand for sustainable alternatives
Lightweight, transparent, flexible
1. The UK Plastics Pact Annual Report 2021-2022

## Slide 4
Polyhydroxybutyrate (PHB)
Bioderived and biodegradable
Semicrystalline polymer
Thermal and barrier properties comparable to conventional plastics
Pure PHB can be brittle due to high crystallinity
Can be tailored through copolymerisation and addition of fillers and plasticisers

## Slide 5
Research Objective
Use molecular dynamics to investigate barrier properties by simulating diffusion of oxygen and water through the amorphous polymer matrix.

## Slide 6
Simulation Method
General Amber Force Field1 (modified)
amorphous polymer
PHB α-crystal
1. Wang, Junmei, et al. Journal of computational chemistry 25.9 (2004): 1157-1174.

## Slide 7
Simulation Method
H2O
O2
1ns NPT equilibration
200ns NVT production run
SPCE model1
Monticelli model2
Berendsen, Herman JC, J. Raul Grigera, and Tjerk P. Straatsma. Journal of Physical Chemistry 91.24 (1987): 6269-6271
Javanainen, Matti, Ilpo Vattulainen, and Luca Monticelli. The Journal of Physical Chemistry B 121.3 (2017): 518-528.

## Slide 8
Post-Simulation Analysis
Mean squared displacement:
r = coordinates
d = dimensionality
N = number of atoms
⟨ ⟩t0 = average over time origins

## Slide 9
Post-Simulation Analysis
Linear regression model used to calculate diffusion coefficient (D)
R2 ≈ 1
Einstein diffusion regime when R2 and log-log slope ≈ 1
from scipy.stats import linregress

## Slide 10
Oxygen Diffusion at 500K
Oxygen diffuses more in 10 monomer system due to chain relaxation timescales

## Slide 11
Oxygen Diffusion at 300K
At 300K diffusion is limited by polymer chain mobility

## Slide 12
Polymer Displacement
Higher D values at higher temperatures due to increased polymer chain mobility
At 300K PHB model is below glass transition temperature
Polymer Chain Mobility

## Slide 13
Water Diffusion at 300K
Water diffusion is slower in 10 monomer system

## Slide 14
Effect of Chain Ends
Dwater lower for 10 monomer chain due to interactions with polar chain ends
Doxygen > Dwater since oxygen is non-polar
3 Å

## Slide 15
Diffusion Coefficient
Permeant | System | Temp (K) | D (cm2/s)
Oxygen | 10 monomers | 500 | 3.76 x10-5
 | 20 monomers | 500 | 2.46 x10-5
 | 10 monomers | 300 | 6.05 x10-8
 | 20 monomers | 300 | 5.45 x10-8
 | Experimental1 | 296 | 5.26 x10-8
Water | 10 monomers | 300 | 1.11 x10-8
 | 20 monomers | 300 | 2.23 x10-8
 | Experimental1 | 298 | 2.17 x10-8
1. Follain, Nadege, et al. The Journal of Physical Chemistry C 118.12 (2014): 6165-6177.
D values in agreement with experiment
Higher D at 500K due to polymer chain mobility
Doxygen > Dwater ; PHB stronger barrier against water
accuracy ± 0.4%

## Slide 16
Comparison to Other Polymers
 | Dwater (x10-8 cm2/s) | Doxygen (x10-8 cm2/s)
PHB | 2.23 | 5.45
PLA1, 2 | 6.61 | 7.6
PET3, 4 | 0.85 | 1.16
1. Yoon, Jin‐San, et al. Journal of applied polymer science 77.8 (2000): 1716-1722.
2. Bao, Lihong, et al. Journal of membrane science 285.1-2 (2006): 166-172.
3. Sammon, C., J. Yarwood, and N. Everall. Polymer 41.7 (2000): 2521-2534
4. Lightfoot, Jasmine C., et al Macromolecules 55.2 (2021): 498-510
PLA = bioderived & biodegradable
PET = petrochemically derived & non-biodegradable

## Slide 17
Conclusions
Permeant polarity and polymer chain mobility determine diffusion properties
Diffusion coefficients from simulations are in agreement with experimental values
PHB is a stronger barrier against water than oxygen
Barrier properties of PHB make it a promising candidate for food packaging applications

## Slide 18
Future Work
Further analysis of H2O and O2 interaction with PHB
Investigate mechanical properties and crystallinity of PHB films
Measure barrier properties using a permeation cell with H2O and O2
Study effect of filler particles and plasticisers

## Slide 19
Acknowledgements
Smart Sustainable Plastic Packaging (SSPP) research group:
Karen Johnston
Paul Mulheran
John Liggat
Vitor Magueijo
Katarzyna Majerczak
Dominic Wadkin-Snaith
To:
Supercomputer resources:
PhD funding:

## Slide 20
X THE PLACE OF USEFUL LEARNING